# Durodek 740 Profile Corrugated Steel

Durodek 740 Profile

The roofing panel shall have a cover width of 740mm. Nominal rib height shall be 29mm. The ribs shall have a nominal pitch of 185 mm center to center and with anti-capillary side lap feature.

#### Steel Grade

The steel cladding shall be roll-formed from high tensile steel in 0.47mm TCT (Total Coated Thickness) where Base Metal Thickness (BMT) is 0.42mm, with minimum yield strength 550N/mm2, metallic hot dip coated with an alloy of 55% aluminum. 43.5% zinc and 1.5% silicon. with 150g/m2 coating mass (AZ150, AS 1397).

Color Coating

Top coat – Advance durability polyester paint of 20m over 5m corrosive inhibit epoxy primer.

Reverse coat – Shadow Grey wash coat of 5m over 5m corrosion inhibitive epoxy primer.

(Factory coiled painted and oven baked to AS2728)

# Flashing

# All flashing shall be manufactured by Roofing Supplier.

# Flashing, capping and trims shall be manufactured from same type or similar standard of finished materials as the profiled steel sheet.

# Galvanized Purlin

The purlin support for the roofing sheet to be Zed Sections of cold-formed steel complying with AS1397-1993.

Steel grade to be G450 (450MPa yield strength), min. Z275 zinc coating (275g/m2 min. coating mass)

# Sealant

Sealants shall be an approved adhesive material, suitable for application on all aspects, of a consistency suitable for application by means of trowel, knife or gun available as a preformed strip or tape for providing a seal between a unit or structure.

The sealant should have the following properties:

- Elasticity to accommodate expected movement of the substrate materials;

- Adhesion to joint surfaces:

- Waterproof;

- Durable to UV light;

- Able to act as an anti-corrosion barrier between dissimilar material;

- When cured, stays rubber from 60 to 200 oC without tearing, cracking, drying out or become brittle;

- Sealant to conform to ASTM C-920 & BS 5889

# Fasteners

Fastener for the roofing sheets & flashing shall be proprietary carbon steel self-drilling and tapping screw recommended by the Roofing Manufacturer.

The coating of the fasteners should comply with AS3566 Class 3 for corrosion resistance. EPDM washer for prevents corrosion and remains elastic for waterproof.

# Quality Assurance

- The roofing installer shall be currently approved by the manufacturer of the roofing material.

- For actual installation of roofing, use only competent and skilled roofer completely familiar with and experienced in the application of the materials specified herein.

- The roofing works shall be carried out by a specialist firm having a minimum 5 years local experience in similar roofing project.