Table of Contents

- Roofing Profiled Sheet

- Flashing

- Purlin (Optional)

- Sealant

- Fasteners

- Quality Assurance

# 1.	Roofing & Walling Profiled Sheet

Profile

The roofing panel shall have  a cover width of 760mm. Nominal rib height shall be 29mm and shall have a nominal pitch of 190mm center to center and with anti-capillary side lap feature.

#### Steel Grade

The steel cladding shall be roll-formed from high tensile steel in 0.54 TCT (Total Coated Thickness) where Base Metal Thickness (BMT) is 0.48, with minimum yield strength 550N/mm2, metallic hot dip coated with an alloy of 55% aluminum. 43.5% zinc and 1.5% silicon.  The coating mass shall be 150g/mm2, total coated both sides as determined by the prescribed triple spot tests (AZ150, AS 1397 –1993).

Clean Colorbond Coating

Top coat – Advance durability polyester paint of 20m over 5m corrosive inhibit epoxy primer.

Reverse coat – Shadow Grey wash coat of 5m over 5m corrosion inhibitive epoxy primer.

(Factory coiled painted and oven baked to AS2728)

Warranty

Material warranty issued from manufacturer for material will have a life prior to perforation by weathering in the natural elements of 10 years. No cracking, flaking or peeling of the paint under warranty period provided the roofing/walling sheets are normally well-washed exposure conditions.

# 2.	Flashing

All flashing shall be manufactured by Roofing Supplier.

Flashing, capping and trims shall be manufactured from same type or similar standard of finished materials as the Trimdek profiled sheet.

# 3.	Thermal & Acoustic Insulation

The thermal & acoustic insulation layer to be 50mm thick, 24Kg/m3 density Fiberglass.

Thermal conductivity of mineral wool: 0.033W/mK at 20oC, U Values – 0.66W/m2K

# 4.     Purlin (Optional)

# The purlin support for the roofing sheet to be Lysaght Zed Sections are roll-formed by Hi-Ten steel complying with AS1397-1993.

Steel grade to be G450 (450Mpa yield strength), Min. Z275 zinc coating (275g/m2 min. coating mass)

All purlins to be fixed with grade 8.8 M 12 / M16 Bolts & Nuts onto the 10mm thick purlin cleats (GMS) which are fixed on the concrete roof by Hilti Anchor Bolts.

# 5.      Sealant

Sealants shall be an approved adhesive material, suitable for application on all aspects, of a consistency suitable for application by means of trowel, knife or gun available as a preformed strip or tape for providing a seal between a unit or structure.

The sealant should have the following properties:

- Elasticity to accommodate expected movement of the substrate materials;

- Adhesion to joint surfaces:

- Waterproof;

- Durable to UV light;

- Able to act as an anti-corrosion barrier between dissimilar material;

- When cured, stays rubber from 60 to 200 oC without tearing, cracking, drying out or become brittle;

- Sealant to conform to ASTM C-920 & BS 5889

# 6.	Fasteners

Fastener for the roofing sheets & flashing shall be proprietary carbon steel self-drilling and tapping screw recommended by the Roofing Manufacturer.

The coating of the fasteners should comply with AS3566 Class 3 for corrosion resistance. EPDM washer for prevents corrosion and remains elastic for waterproof.

# 7.	Quality Assurance

  - The roofing installer shall be currently approved by the manufacturer of the roofing material.

  - For actual installation of roofing, use only competent and skilled roofer completely familiar with and experienced in the application of the materials specified herein.

  - The manufacturer shall be an ISO 9002 accredited company.

  - The roofing works shall be carried out by a specialist firm having a minimum 5 years local experience in double standing seam roofing project.